Material properties:

- Density : 8910 kg/m^3

- Young Modulus : 75.854 GPa

- Poisson’s Ratio : 0.34

- Bulk Modulus : 79.015 GPa

- Shear Modulus : 28.304 GPa

Simulated modal analysis ANSYS in AIR (free boundary condition)

Experimental modal analysis in AIR (free boundary condition)

| Mode | Natural frequencies (Hz) |
| --- | --- |
| 1 ND | 191.6 |
|  | 192.8 |
| Torsion | 226 |
| 2 ND | 293.625 |
|  | 299.125 |
| 3 ND | 703.25 |
|  | 712 |
| 4 ND | 1310.875 |
|  | 1320 |